## Slide 1: DECAY AND SAFETY THE DIGITAL CAPTURE OF FILM
dt culturalheritage west coast roundtable
march 2019
Overseas Weekly collection, Hoover Institution Library and Archives
Notes: 1st time here at a round table, looking forward to…
Digital capture of deteriorating film has many challenges.
hybrid photograph conservation / digitization company
many unusual and challenging deteriorated film projects

## Slide 2: Overview
Film deterioration and health hazards
Care and capture of deteriorated film:
  What you can do TOMORROW
  What you can do LONG-TERM
  What you can OUTSOURCE
Notes: Focus on:
typical deterioration issues and solutions
health and safety concerns
And how you might approach these:
TOMORROW & LONG-TERM
And what you might OUTSOURCE (to your conservation lab or to a vendor)

## Slide 3: Film cross-sections
Anti-curl layer (gelatin)
Film base (plastic)
Silver particles in gelatin
Color dyes in gelatin
B+W film
Color film
Notes: A good starting point is the structure of films–
since each component has its own weaknesses in terms of long-term preservation.

## Slide 4
Film base
  Cellulose nitrate
  Cellulose acetate
Image
  Silver
  Color dyes
Image Binder
  Gelatin
Decomposes
Discolors / fades / mirrors
Fades
Grows mold
Film deterioration

## Slide 5
Film becomes:
Toxic!
Embrittled
Yellow
Sticky
Non-existent
Nitrate film-base decomposition
Nitrogen Dioxide Exposure Symptoms: irritation of eyes, nose, throat; cough; mucoid frothy sputum, decreased pulmonary function, chronic bronchitis, dyspnea (breathing difficulty); chest pain; pulmonary edema, cyanosis, tachypnea, tachycardia
Portrait of Jean Arthur, UCLA Special Collections
Notes: Toxic
When it deteriorates, it’s VERY bad
Nitrate film is like the little
girl of the old nursery rhyme:
There Was a Little Girl
There was a little girl, Who had a little curl, Right in the middle of her forehead. When she was good, She was very good indeed, But when she was bad she was horrid. -- Henry Wadsworth Longfellow

## Slide 6
Acetate film-base decomposition
Film becomes:
Toxic!
Acidic
Embrittled
Shrunken
George Hunter, cellulose acetate negative, Library and Archives Canada
Notes: Toxicity study published by the Arizona State Museum in 1987 “Deteriorating Negatives: A Health Hazard in Collection Management”
Personal injuries occurred during handling of nitrate and acetate films during duplication project.

## Slide 7
Color dye fading
Late 1940s 5” x 7” color transparencies
GWAC study collection
Notes: An important form of deterioration– but not related to human safety

## Slide 8
Silver image oxidation
Silver image particle breakdown:
Silver-mirroring
Fading
Lewis Hine, George Eastman Museum
Notes: Typical highlight fading / loss of detail in gelatin silver prints not typically seen in B+W negatives
Silver mirroring is certainly seen, but doesn’t generally cause any issues in transmissive digital capture

## Slide 9
1906 Earthquake negatives
Mold and water damage
Private Collection
Notes: Mold growth on gelatin can completely destroy or just weaken an image
Mold breaks down gelatin’s complex triple helix / polymer structure allowing it to dissolve rather than gel in water
Changing solubility means that cleaning it is much riskier

## Slide 10
Protect Film w/ DT Film scanning kit
Avoid curved film path or rigid film holders in dedicated film scanners (e.g. Flextight, Coolscan)
Avoid heat
Avoid pressure
Keep negative visible / under your control at all times
AN or AR glass / spacers
What you can do: TOMORROW
Notes: Protect Film Physically

## Slide 11
Maximize capture quality and information retention
Capture negative as negative (C1 optimizes this workflow)
Dust removal
  Rocket bulb
  Anti stat gun
  Kinetronics StaticVac and similar
What you can do: TOMORROW
Iron-based developer
Andrew Russell wet collodion negative, Oakland Museum
Notes: What DT calls OBJECT REPRODUCTION MASTER vs CONTENT REPRODUCTION MASTER
Often older/deteriorated film materials are even more important to capture as AS THEY ARE
Good general practice for CH materials, but even more important with older negative materials
--Shows important process characteristics– such as developer and fixer types
--Distinguishes clearly between Deterioration and Image
Andrew Russell wet plate negatives are an extreme example (not film-based) of when showing the original negative is important for scholars in understanding his work

## Slide 12
IRON
PYRO
Notes: OMCA went further and documents transmissive and reflective images of Andrew Russell negatives
Ferrous Sulfate
Fast acting
Less dense negative, often required intensification for printing out papers
Clear shadows
Pyrogallic Acid
Slower acting (restrained to reduce fogging with long development)
Builds greater density, good for printing out papers
More detail in shadows and denser highlights

## Slide 13
What you can do: TOMORROW
Maximize capture quality and information retention
Capture negative as negative (C1 optimizes this workflow)
Dust removal
  Rocket bulb
  Anti stat gun (caution)
  Kinetronics StaticVac and similar
Notes: Deteriorated negative = dusty often from brittle enclosures

## Slide 14
What you can do: TOMORROW
Protect yourself
Avoid fumes
  Ventilation/air exch. (?)
  Elephant trunks (?)
  Full-face respirators (?)
  Fume hoods (!)
Limit quantity of film
Nitrile gloves
Air-out before handling
Notes: pictur

## Slide 15
What you can do: TOMORROW
Protect yourself
Avoid fumes
  Ventilation/air exch. (?)
  Elephant trunks (?)
  Full-face respirators (?)
  Fume hoods (!)
Limit quantity of film
Nitrile gloves
Air-out before handling
Notes: For smaller quantities nitrile gloves/ and a mask or elephant trunk may be sufficient
(no guarantees– that’s between you and your Industrial Hygienist)
Larger quantities REQUIRE fume hood

## Slide 16
Rehouse in archival enclosures
Digitize
Freeze
What you can do: LONG-TERM
Notes: Order of operations:
Wrong way: slowly reorganize, Resleeve, digitize, and freeze
Right way: Freeze, then slowly digitize
Consider a perfect archival storage room full of acetate and nitrate
Normal archival standards for documents do not apply!

## Slide 17
Freeze first, then digitize
Freezing has many benefits
  Slows all deterioration
  Eliminates harmful off gassing
  Inexpensive (relatively)
  Gives you time
What you can do: LONG-TERM
Notes: Don’t need fancy clean archival boxes

## Slide 18
Art Institute of Chicago
Cold Storage Vault
What you can do: LONG-TERM
Freeze first, then digitize
Freezing has many benefits
  Slows all deterioration
  Eliminates harmful off gassing
  Inexpensive (relatively)
  Gives you time
Notes: Art Institute of Chicago– first photo cold storage vault in the work

## Slide 19
All deteriorated acetate or nitrate
Acetate emulsion stripping
Separating stuck film
Tape removal
Cleaning of negatives
Other risky treatments
Deteriorated film: OUTSOURCE
Notes: Some of this you may be able to do in-house with the right staff or with some consulting.
But given the challenges and toxicity of nitrate and acetate, you may choose to outsource all of it.

## Slide 20
Deteriorated film: OUTSOURCE
All deteriorated acetate or nitrate
Acetate emulsion stripping
Separating stuck film
Tape removal
Cleaning of negatives
Other risky treatments
Notes: With nitrate sometimes there’s only so much that can be saved

## Slide 21
Deteriorated film: OUTSOURCE
All deteriorated acetate or nitrate
Acetate emulsion stripping
Separating stuck film
Tape removal
Cleaning of negatives
Other risky treatments
Notes: With Acetate, even extreme vinegar syndrome can usually be recovered from….at a cost.
Cost of emulsion stripping -- one reason why freezing is less expensive

## Slide 22: Plasticizer exudation from degrading film
Phthalate plasticizers
Liquid-filled bubbles

## Slide 24
Notes: Acetic acid is a weak acid and does not attack gelatin or silver
Treatment is possible

## Slide 25
Notes: Show & Tell: stripped pellicle

## Slide 26
Notes: Minor White by Rose Mandel
One of her teachers at the California School of Fine Arts (now SFAI) where she studied photography

## Slide 27
Notes: Minor White by Rose Mandel
One of her teachers at the California School of Fine Arts (now SFAI) where she studied photography

## Slide 28
Deteriorated film: OUTSOURCE
All deteriorated acetate or nitrate
Acetate emulsion stripping
Separating stuck film
Tape removal
Cleaning of negatives
Other risky treatments
Notes: Whether film to paper or film to film the negatives can sometimes be saved

## Slide 29
Deteriorated film: OUTSOURCE
All deteriorated acetate or nitrate
Acetate emulsion stripping
Separating stuck film
Tape removal
Cleaning of negatives
Other risky treatments
Notes: Water-activated, pressure-sensitive, rubber cement– many kinds of tapes and adhesives have been used.
Sometimes they obscure image.

## Slide 30
Black paper tape with water-activated adhesive used during print production
Often covered image
Safely removed with humidification by poultice or damp blotters & Gore-Tex
Conservation: tape removal
PPIE, Cirkut panorama, Bancroft Library
Notes: Emulsion stripping is a fairly extreme treatment to save negatives.
Most of the time simple cleaning or tape removal is sufficient
REVEAL the image by cleaning, rather than digitally fix later.
Cleaning improves image quality, saves time, and preserves the negative by removing dirt and accretions that can cause damage over time.
Though we do plenty of work that is just conservation or just digitization, some of our most satisfying projects are when we can do both– conservation cleaning, tape removal, flattening, etc and THEN rapid digital capture.

## Slide 31
Black paper tape with water-activated adhesive used during print production
Often covered image
Safely removed with humidification by poultice or damp blotters & Gore-Tex
Conservation: tape removal
PPIE, Cirkut panorama, Bancroft Library

## Slide 32
Deteriorated film: OUTSOURCE
All deteriorated acetate or nitrate
Acetate emulsion stripping
Separating stuck film
Tape removal
Cleaning of negatives
Other risky treatments
Notes: Cleaning of negatives is a whole lecture in and of itself…water, alcohol, other organic solvents…
The trick is dissolving the dirt but not the negative…
And deteriorating negatives have altered solvent sensitivities as they chemically decay, so each one is a little different.

## Slide 33
Deteriorated film: OUTSOURCE
All deteriorated acetate or nitrate
Acetate emulsion stripping
Separating stuck film
Tape removal
Cleaning of negatives
Other risky treatments

## Slide 34
Notes: Stay in touch with my very occasional newsletter…

## Slide 35
gawainweaver.com • twocatdigital.com
gw@gawainweaver.com
18 Greenfield Avenue, San Anselmo, CA 94960
415-446-9138